## Slide 1
Lecture 3 – Materials and Molecules Generation
김지한 (카이스트)
8.20.2021

## Slide 2: Materials and Inverse Design
One of the major goals in computational materials design is the concept of inverse design.
Inverse design: Property goal → Material (as opposed to materials → property).

## Slide 3: Molecules/Materials Representation Revisited

## Slide 4: SMILES and Molecule Generation
From paper: Automatic Chemical Design Using a Data-Driven Continuous Representation of Molecules
The authors transformed SMILES (discrete representation) into a continuous vector and used something called autoencoder to generate new molecules.
To show how this is done, we again take a look at the MNIST example.

## Slide 5: From Molecules to Materials
One can think that generating materials will be something similar to generating molecules.
That is, we can start with the SMILES representation of the materials and then proceed to generate new materials via VAE.
One problem is that materials (crystalline) are pretty much infinite so it becomes problematic to represent them in SMILES.
Also, with materials, the lattice parameters matter greatly and somehow this information needs to be encoded.
Moreover, materials need to abide by the strict periodic boundary conditions whereas molecules do not need to worry about periodic boundary conditions.

## Slide 6: Introduction to Nanoporous Materials
Zeolites
Metal-organic frameworks
(MOFs)
Nanoporous materials: contain pores on the order of few Angstroms to nanometers.
Different classes of materials exist: zeolites, MOFs, COFs, etc.
Large surface area and high tunability.
Covalent organic frameworks (COFs)

## Slide 7: Potential Applications of Nanoporous Materials
Gas Separation
(e.g., carbon capture, pollutant removal)
Sensor
Gas Storage
(e.g. H2/CH4 storage, ANG vehicle)
Catalysis
P. Kumar et al, TrAC 73, 39 (2015).
Z. Hu et al., Chem. Soc. Rev. 43, 5815 (2014).
S.M. Auerbach et al., “Handbook of zeolites science and technology”, CRC press (2003).
D.M. D’Alessandro et al., Angew. Chem. Int. Ed. 49, 6058 (2010).
N.A. Khan et al., J. Hazard Mater. 244-245, 444 (2013).
J.A. Mason et al., Chem. Sci. 5, 32 (2014).
M.P. Suh et al., Chem. Rev. 112, 782 (2011).
Porous
Materials

## Slide 8: Can Artificial Intelligence (AI) Generate New Porous Materials?
Basic Idea: millions of materials (e.g. zeolites, MOFs, polymers) exist
Existing zeolites, MOFs, polymers  feed into artificial neural network (ANN)
After training on thousands (millions) of materials, can AI generate new materials?
??
Library of Existing Materials Some Neural Network New Materials
8

## Slide 9: AI Generating Human Face
www.thispersondoesnotexist.com

## Slide 10: Generating Human Faces vs Generating Materials

## Slide 11: Pure-silica Zeolites
Porous material: pure-silica (Si, O) zeolites
  Experimentally determined zeolites (IZA): 234 zeolites
  Computationally discovered zeolites (PCOD): ~330,000 zeolites
Target property: methane (CH4) adsorption
  Training set: ~30,000 zeolites
  Test set: ~30,000 zeolites
Zheng, Y., Li, X. & Dutta, P. K. Sensors 12, 5170–5194 (2012).

## Slide 12: Case Study Application: Adsorbed Natural Gas (ANG) Vehicles
Recently, US DOE was interested in the adsorbed natural gas (ANG) vehicle technology.
Compared to the compressed natural gas (CNG) vehicle, the storage is at mild conditions (T = 298 K, P = 35-65 bar).
The DOE target for ANG was set at methane working capacity of 315 cm3/cm3, which would make ANG comparable to CNG.
However, after years of research (i.e. millions of dollars spent), the best material only has around working capacity of 200 cm3/cm3.
??
CNG
ANG

## Slide 13: Which ANN? Generative Adversarial Network (GAN)
Most popular generative ANN (developed in 2014)
GAN has two main neural networks (Discriminator and Generator); Example
https://www.kdnuggets.com/2016/07/mnist-generative-adversarial-model-keras.html
Random Noise
Generative
Model (Thief)
Discriminative
Model (Police)
Real or Fake?
Fake Money
Real Money

## Slide 14: Objective of the Zeolite Project
1) A generative model for zeolites
2) Fine tuning of user-desired adsorption property
+
ANN
Material/property
representation
ANN Architecture
for this representation
Porous material
generation
18-22 kJ/mol
19 kJ/mol
ANN

## Slide 15: No Representations for Crystalline Material Generation Using Artificial Intelligence
16
Lattice information
(a, b, c, α, β, γ)
Periodic boundary conditions
DIFFICULT!!
EASY!!

## Slide 16: 3D Shape(Grid) Representations
Energy shape
Material shape (O)
Material shape (Si)
Adsorption properties
(KH, heat of adsorption, …)
Atomic positions
)
Lennard-Jones potential
Gaussian

## Slide 17: Generative Adversarial Network for Zeolites (ZeoGAN)
*S. Lee et al., Journal of Materials Chemistry A 7, 2709 (2019).
*B. Kim et al., Science Advances 6, eaac9324, (2020).

## Slide 18: Convergence of ZeoGAN
Earth-Mover Distance (EMD)
distance between Real/Generated data distributions
determines when to stop the neural network simulations

## Slide 19: Zeolite Cleanup Algorithm

## Slide 20: Generated Zeolites Statistics
1 million zeolite-like shapes were generated.
Only ~120 fit the criterion of real zeolites (Si:O = 0.5, all the bond types/lengths/angles reasonable).
There is still much work to be done to improve the statistics.

## Slide 21: Generated Zeolites vs. Existing Zeolites

## Slide 22: Is Inverse Design Possible in Our Work?
Material design today
Inverse design using AI
Synthesis/
Generation
Testing
Material
Concept
AI

## Slide 23: Generated User-desired Zeolites
Energy Shape
Heat of adsorption
User-desired loss
(18 to 22 kJ/mol)

## Slide 24: Generated User-desired Zeolites
Target heat of adsorption value: 18 ~ 22 kJ/mol

## Slide 25: Zeolites vs MOFs (a.k.a. Coordination Polymers)
Nanoporous materials: contain pores on the order of few Angstroms to nanometers.
Different classes of materials exist: zeolites, MOFs, COFs, etc.
Large surface area and high tunability.
Zeolites
Metal-organic frameworks
(MOFs)
Crystalline
Porous
Chemically Simple (pure silica)
Crystalline
Porous
Chemically Complex

## Slide 26: Number of MOFs is Increasing Rapidly
The number of MOFs is increasing rapidly (Over 70,000 experimentally synthesized MOFs and many more number of hypothetical materials exist).
Big data set does exist even for just the experimental structures.
Experimental MOFs

## Slide 27: Different Representation of MOFs
Metal cluster
Organic linker
MOF
One of the key features of MOFs is its modularity.
There are hundreds of different metal clusters and hundreds of different linkers.
And they can be built in a facile manner for different combinations.
So we will use these “components” as a single cluster in representation for the AI.

## Slide 28: MOFs - Combinatorial Lego Building Blocks
C. Wilmer et al., Nat. Chem. 4, 83 (2012).

## Slide 29: Node/Edge Abstraction for MOFs
The unit cell of each of these MOFs can be abstracted into node, edge, and known topologies. Example

## Slide 30: Topology for Different MOFs
There are more than 3000 topologies reported in the RCSR database.

## Slide 31: Node x Edge x Topology = Trillions of Possible MOFs
648 Node x 219 edge x 1775 topologies → 2.47 x 1014 Possible MOFs!!
This materials space is much larger than the 70,000 experimentally synthesized MOFs.

## Slide 32: Component #1. Genetic Algorithm
Chromosome
Crossover operation

## Slide 33: Component #2: MOF-NET

## Slide 34: MOF-NET Performance for Methane Storage
MAE: mean absolute error
RMSE: root-mean-square error

## Slide 35: Distribution of MOFs with Methane Working Capacity (WC)

## Slide 36: Prediction of Record Breaking MOFs
*964 MOFs

## Slide 37: Top Candidate MOFs